Project Title:

Conversion of post-combustion gas from cement manufacturing to syngas by electrochemical CO2 capture and reduction

……..........................................................

Dr. Pongkarn Chakthranont

Sothearoth Heng

NCR ID: 803198

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2024-22237-EN

March 2025

March monthly report

- Tasks list for March

- Optimization of the 25cm2 CO2 electrolyzer operating condition:

  - Torque force

  - Cathodic/Anodic flow rate

  - Current density

- CO2 electrolysis under a pure CO2 at 200mA/cm2 in AEM electrozer system

- Experimental Procedure

Membrane electrode assembly set-up

A 25 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The Ni foam (5.4 x 5.4 cm), bipolar membrane (BPM, 6 x 6 cm), and NiSAC (5 x 5 cm) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled and tightened with a torque force of 35 inch-lbs. 200 ml of 1M KOH was recirculated and used throughout the experiment as the anolyte at 25 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 150 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Influence of applied current density on CO2RR performance

Studying the impact of the applied current density in CO2 electrolysis is crucial as it directly influences the product selectivity, energy efficiency, and overall system performance. The figure 1. Illustrates the CO2 electrolysis under a pure CO2 at 100 – 175 mA/cm2. The overall system enables to sustain a high CO selectivtiy with FE(CO) > 93% at applied current density range of 100 – 175mA/cm2 with a rising overpotential as current density increases from 3.65V at 100mA/cm2 to 5.91V at 175mA/cm2. Furthermore, it is worth noting that once further ramping the current density to 200mA/cm2, we observed a significant drop in CO selectivity with an overshoot cell voltage which could be attributed to either cell failure or electrode degradation at such a high current density. Therefore, further improvement on the overall system such as increasing the catalyst mass loading of the cathode and using IrO2 anode should be considered.

Figure 1. CO2 electrolysis of a zero-gap MEA (Ni foam/BPM/NiSAC) under a pure 300ml/min CO2 and 25ml/min of 1M KOH at 100 – 175 mA/cm2

Short-term CO2 electrolysis of NiSAC under a pure CO2 condition at 100mA/cm2

To preliminarily determine the stability of the 25cm2 electrolyzer with a similar cell configuration and operating condition to 5cm2 electrolyzer, the short-term CO2 electrolysis was experimentally conducted. As can be seen in Fig. 2, the 25cm2 electrolyzer with 1.6mg/cm2 NiSAC cathode exhibits a very great performance with FE(CO) > 97% with a slightly high cell voltage of 4.15V over 6hours. According to these results, we hypothetically assume that the NiSAC mass loading could somehow impact the overpotential of the overall cell system but not catalytic performance.

Figure 2. CO2 electrolysis of a zero-gap MEA (Ni foam/BPM/Ni0.5SAC) under a pure 300ml/min CO2 and 25ml/min of 1M KOH at 100mA/cm2

CO2 electrolysis in AEM system under a pure CO2 condition at 200mA/cm2

In order to evaluate the feasibility of operating a 25 cm² AEM electrolyzer for CO₂ electrolysis at a higher current density with minimal cell voltage, a cell configuration with an anion exchange membrane was deployed and operated under a pure CO₂ flow of 150 mL/min at 200 mA/cm². The overall system was able to sustain CO selectivity similar to that of a BPM electrolyzer, achieving a maximum FE(CO) > 97% with a lower cell voltage of 2.85V. Despite its superior performance in minimizing cell voltage, the AEM electrolyzer demonstrated poor stability due to massive salt buildup during the reaction, leading to cell failure after 40 minutes of operation. However, it is worth noting that the stability of the AEM system can be improved by using a highly diluted electrolyte concentration, a cesium-based electrolyte, and optimized cell temperature, all of which could potentially mitigate cation accumulation at the cathode side over time.

Figure 3. CO2 electrolysis of a zero-gap MEA (Ni foam/AEM/Ni0.5SAC) under a pure 150ml/min CO2 and 25ml/min of 1M KOH at 200mA/cm2

- Upcoming tasks

- Influence of catalyst mass loading on the overall cell performance

- Influence of different total CO2 flow rates on the overall cell performance

- CO2 electrolysis under a pure CO2 at 200mA/cm2

- Preparation of IrO2-TiPt (5.4 x 5.4 cm2) anode