โครงการ P2451496 งบยุทธ_CCU68_การต่อยอดและพัฒนาเทคโนโลยี Carbon capture and utilization (CCU) ที่มีความต้องการจากภาคอุตสาหกรรม และขับเคลื่อน National CCUS Alliance ร่วมกับเครือข่ายพันธมิตร

Sothearoth Heng

Under the supervision of

Dr. Pongkarn Chakthranont

ใบสั่งจ้างเลขที่ PO25005060

จ้างเหมาพัฒนางานจ้างพัฒนาการขยายขนาดเซลล์ไฟฟ้าเพื่อการผลิตแก๊สสังเคราะห์จาก CO2 เชิงเคมีไฟฟ้า

งวดที่ 1: 1 เมษายน 2568 – 31 เมษายน 2568

……..........................................................

Dr. Pongkarn Chakthranont

April monthly report

- To-do list for April

- Optimization of 25cm2 CO2 electrolyzer operating condition:

  - Influence of catalyst mass loading on the overall cell performance

  - Influence of different total CO2 flow rates on the overall cell performance

- Stability test of Ni0.25SAC under diluted 15%CO2/85%N2 and pure CO2 conditions using 5cm2 CO2 electrolyzer

- Experimental Procedure

Membrane electrode assembly set-up

A 25 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The Ni foam (5.4 x 5.4 cm), bipolar membrane (BPM, 6 x 6 cm), and NiSAC (5 x 5 cm) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled and tightened with a torque force of 35 inch-lbs. 200 ml of 1M KOH was recirculated and used throughout the experiment as the anolyte at 25 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 150 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Influence of applied current density on CO2RR performance

Studying the impact of the applied current density in CO2 electrolysis is crucial as it directly influences the product selectivity, energy efficiency, and overall system performance. The figure 1. Illustrates the CO2 electrolysis under a pure CO2 at 100 – 200 mA/cm2. The overall system enables to sustain a high CO selectivtiy with FE(CO) > 91% at applied current density range of 100 – 200 mA/cm2 with a rising overpotential as current density increases from 3.65V at 100mA/cm2 to 6.37V at 200mA/cm2. Furthermore, it is worth noting that once further ramping the current density to 200mA/cm2, we observed a significant increase in cell voltage with a marginal drop of FE(CO) which could be attributed to either cell failure or electrode degradation at such a high current density.

Figure 1. CO2 electrolysis of a zero-gap MEA (Ni foam/BPM/NiSAC) under a pure 300ml/min CO2 and 25ml/min of 1M KOH at 100 – 200 mA/cm2

Influence of catalyst mass loading on CO2RR performance

In order to evaluate the effect of catalyst layer (CL) thickness on the overall performance of the NiSAC, here we conducted the CO2 electrolysis under a pure CO2 condition at 100mA/cm2 with different NiSAC mass loading of 1.6, 2.1, and 2.5 mg/cm2. As depicted in Fig. 2, the overall cell performance in terms of CO selectivity and cell voltage exhibited similar results at different mass loading, thereby showing a slight impact of the catalyst mass loading on the cell performance. A mass loading of 2.1 mg/cm² provides the best balance of high CO selectivity and energy efficiency under the given experimental conditions. Increasing the mass loading beyond this point (to 2.5 mg/cm²) leads to a slight decrease in CO selectivity and an increase in voltage, which may indicate mass transport limitations at higher loadings. Based on these results, a NiSAC with mass loading of 1.80.3 mg/cm2 will be selected for further investigation.

Figure 2. CO2 electrolysis of Ni0.5SAC with m/l of 1.6, 2.1, and 2.5 mg/cm2 under a pure 300ml/min CO2 and 25ml/min of 1M KOH at 100 mA/cm2

Influence of different CO2 flow rates on CO2RR performance and single-pass CO2 utilization (SPU)

Understanding the impact of CO₂ supply on CO selectivity and SPU is critically important for experimental design aimed at achieving maximum CO selectivity while maintaining high carbon efficiency. Figure 3 illustrates the influence of CO₂ supply on both CO selectivity and SPU. Across all CO₂ flow rates, the system consistently achieved high FE(CO) > 94%, with a maximum SPU of 36% at a CO₂ flow rate of 50 ml/min. This highlights a trade-off, where lower CO₂ flow rates offer significantly higher single-pass CO2 utilization while preserving product selectivity.

Figure 3. CO2 electrolysis of Ni0.5SAC under a pure 50, 150, and 300ml/min CO2 and 25ml/min of 1M KOH at 100 mA/cm2

Long-term CO2 electrolysis of NiSACs (0.25, 0.5, 1, and 2) under diluted and pure CO2 conditions at 100mA/cm2

Figure 4 illustrates the long-term CO2 electrolysis for CO production during CO₂ electrolysis, utilizing various nickel single-atom catalysts (NiSACs): Ni0.25SAC, Ni0.5SAC, Ni1SAC, Ni2SAC, and Acid-Ni0.5SAC. These catalysts were tested in a diluted gas mixture of 15%CO₂/ 85% N₂ at a constant current density of 100 mA/cm². Among the tested catalysts, Ni0.25SAC exhibited the most stable and sustained performance, consistently surpassing 80% CO FE throughout an extended 80-hour operation. Ni0.5SAC initially achieved a higher FE (~88%) but gradually declined over time. Ni1SAC, Ni2SAC, and Acid-Ni0.5SAC exhibited similar outcomes to Ni0.5SAC, commencing with a higher initial FE(CO) (~90%) before experiencing rapid losses in CO selectivity within the first 10 hours.

Key Observations:

Effect of Nickel Loading

Lower Loadings (Ni0.25SAC and Ni0.5SAC): These catalysts maintain higher efficiencies over time compared to higher loadings. Ni0.25SAC, having the lowest nickel content, exhibits the best performance, maintaining efficiency near 90% over 80 hours. Ni0.5SAC shows a slight decline in terms of selectivity but still maintains it above 65% over 35 hours.

Higher Loadings (Ni1SAC and Ni2SAC): For higher loadings, the increased nickel content seems to compromise long-term stability, as these catalysts suffer rapid and significant FE(CO) drops early in the process.

Impact of Acid Treatment: The acid-treated Acid-Ni0.5SAC initially performs like Ni0.5SAC, with a slightly higher FE(CO), but its efficiency declines more rapidly. This suggests that acid treatment negatively impacts long-term performance, possibly by increasing the catalyst's surface hydrophilicity, which leads to rapid GDE flooding.

Figure 5 presents the long-term CO₂ electrolysis performance of Ni0.25SAC and Ni0.5SAC catalysts at a current density of 100 mA/cm². Ni0.25SAC consistently maintains a high and stable CO selectivity, with an average FE(CO) approx. 94% over the 90-hour operation. This demonstrates exceptional selectivity and durability. In contrast, Ni0.5SAC initially exhibits comparable performance with a slightly higher FE(CO) approx. 97% but gradually declines after 70 hours. Furthermore, Ni0.25SAC operates at a lower and more stable cell voltage than Ni0.5SAC, reflecting increased energy consumption and diminished system stability over time. These findings underscore Ni0.25SAC as the more efficient and stable catalyst for sustained CO₂ electrolysis under both diluted 15%CO2/85% and pure CO₂ conditions.

Figure 4. CO2 electrolysis of Ni0.25SAC (m/l = 1.80.1mg/cm2) under 100ml/min of 15%CO2/85%N2 and 8ml/min of 0.25M KOH at 100 mA/cm2

Figure 5. CO2 electrolysis of Ni0.25SAC and Ni0.5SAC (m/l = 1.80.1mg/cm2) under a pure 150ml/min CO2 and 8ml/min of 0.25M KOH at 100 mA/cm2

- Upcoming tasks

- 25cm2 electrolyzer - Stability of Ni0.25SAC (m/l = 1.80.2mg/cm2) with 0.25M - IrO2 under 300ml/minCO2 at 100mAcm2

- 25cm2 electrolyzer - Stability of Ni0.25SAC (m/l = 1.80.2mg/cm2) with 0.25M - IrO2 under 30ml/minCO2 at 100mAcm2