……..........................................................

Dr. Pongkarn Chakthranont

โครงการ P2451496 งบยุทธ_CCU68_การต่อยอดและพัฒนาเทคโนโลยี Carbon capture and utilization (CCU) ที่มีความต้องการจากภาคอุตสาหกรรม และขับเคลื่อน National CCUS Alliance ร่วมกับเครือข่ายพันธมิตร

Sothearoth Heng

Under the supervision of

Dr. Pongkarn Chakthranont

ใบสั่งจ้างเลขที่ PO25005060

จ้างเหมาพัฒนางานจ้างพัฒนาการขยายขนาดเซลล์ไฟฟ้าเพื่อการผลิตแก๊สสังเคราะห์จาก CO2 เชิงเคมีไฟฟ้า

งวดที่ 7: 1 October 2568 – 30 October 2568

October monthly report

- To-do list in October

  - 100cm2 MEA electrolyzer – CO2 electrolysis of serpentine-BPM system under a dried 200ml/min CO2, 100ml/min of 0.25M KOH, and IrO2-TiPt anode at 100mA/cm2

  - 100cm2 MEA electrolyzer – CO2 electrolysis of serpentine-BPM system under a humidified 200ml/min CO2, 100ml/min of 0.25M CsOH, and IrO2-TiPt anode at 100mA/cm2

- Experimental Procedure

Synthesis of NiSAC by pyrolysis method

The synthesis of NiSAC catalyst was followed by our previous work. Initially, nickel phthalocyanine (NiPc), urea, and dicyanamide precursors were stoichiometrically weighed according to mass ratios of x:5:5, wherein urea and dicyanamide were maintained at 5 g each while varying the NiPc content (x = 0.25, 0.5, 1.0, and 2.0 g). Subsequently, the mixture was thoroughly mixed and ground until a homogeneous midnight blue powder was obtained. The fine powder was then transferred into a quartz boat covered with a capsule lid and subjected to polymerization at 800 °C (ramp rate = 10 °C·min⁻¹) in a horizontal tube furnace under an argon atmosphere (flow rate = 200 sccm) for 2 h. The as-prepared xNiSAC catalysts with different NiPc contents were finally obtained and labeled as 0.25NiSAC, 0.5NiSAC, 1.0NiSAC, and 2.0NiSAC.

Fabrication of IrO2/TiPt felt anode electrode

The IrO2/TiPt-felt anode electrode was prepared using a thermal deposition method involving multiple sequential steps. Initially, the TiPt felt (Purchased from ...) substrate was ultrasonically cleaned with deionized water and acetone to remove any surface contaminants. The cleaned substrate was subsequently etched in a 6M HCl solution at 90°C for 45 min to enhance surface roughness and adhesion properties. The dip-coating solution was prepared by dissolving 200 mg of IrCl6·xH2O in 18 mL of isopropanol (IPA) containing 10% v/v HCl (2 mL of conc. HCl). The etched TiPt felt substrate was then immersed in the dip-coating solution, followed by drying at 100°C for 5 min in an oven and subsequent calcination at 500°C for 10 min in a muffle furnace. After cooling to room temperature, the treated substrate was reweighed to determine mass gain. This dipping-drying-calcination cycle was repeated several times until the desired IrO2 mass loading (10.2 mg/cm2) was achieved.

Preparation of NiSAC cathode electrode via spray coating method

The NiSAC gas-diffusion electrode was fabricated by spray coating onto Sigracet 39BB carbon paper or hydrophilic carbon cloth substrates. Typically, 150 mg of as-prepared NiSAC and 381 μL of XC-2 ionomer were ultrasonically dispersed in 10 mL of isopropanol (IPA) for at least 1 h to form a homogeneous dark colloidal suspension. The ink suspension was subsequently spray-coated onto a 11 x 11 cm2 carbon substrate using an automated, custom-built spraying setup equipped with a syringe pump operating at a flow rate of 0.6 mL min⁻1 on a hotplate maintained at 130°C, yielding a catalyst mass loading of 1.8 ± 0.1 mg.cm⁻2.

Note: a bottle of ink suspension containing 150mg of Ni-SAC catalyst yields only ~ 0.7 ± 0.1 mg.cm⁻2.

Electrochemical measurements in membrane-electrode assembly (MEA) electrolyzer

100cm2 MEA electrolyzer operational set-up

A 100 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The Ni foam or IrO2-TiPt felt (10.5 x 10.5 cm2), bipolar membrane (BPM, 15.6 x 16.8 cm2), and 0.5Ni-SAC (10.5 x 10.5 cm2) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled with 0.25µm PTFE gasket and tightened at a compression force of 25 Nm. 1.0 L of 0.25 M KOH was recirculated and used throughout the experiment as the anolyte at 100 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 200-1000 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Influence of dried-CO2 gas stream and acid humidified + CsOH

Dried-CO2 gas steam: According to our previous results on studies of different types of flow-field channels, we demonstrated that the cathodic quad-serpentine flow-field channel worked best for the CO2RR in the 100cm2 BPM electrolyzer at 100mA/cm2 due to improved CO2 distribution and minimized stagnant zone in the flow-field. However, the accumulated droplets remained still in the serpentine flow-field. Therefore, we attempted to utilize dried-CO2 gas stream instead of humidified-CO2 gas stream in the aim of reducing accumulated water as much as possible. As shown in Figure 1b (green line), the BPM electrolyzer operated under dried-CO2 condition failed faster than humidified-CO2 condition (orange line) with an abruptly drop in FE(CO) to 80% after 8hr of the operation. Furthermore, the water accumulation remained the same as the humidified-CO2 condition, while the precipitated salt is vividly observed at the cathodic inlet. this result revealed that the accumulated droplets might come from the in-situ H2O generation between H+ from CEL and OH- from CO2RR byproduct or the KOH electrolyte leakage thru the gasket due to insufficient compression force and thinner gasket.

Acid humidified-CO2 and CsOH: According to the previous results, we observed both accumulated droplets and precipitated salt in the cathodic flow-field channels which were likely the reasons of cell failure. To identify the main root cause of cell dying, we hypothetically neglected the effect of accumulated droplets and considered the salt precipitation is the main driving force of cell dying. We replaced the KOH anolyte with the CsOH solution as it is well-known for low Cs+ crossover rate due to its large ionic radius than K+, and utilized 50mM CH3COOH solution as a humidifier instead of DI water. As shown in Figure 1b (blue line), The system exhibited similar way of cell failure to the previous system operated with KOH electrolyte by sustaining the FE(CO) around 85% over 10hr of the operational duration. this finding suggested that accumulated salt at cathode might not be the main reason of cell dying in this early stage of cell operation. Therefore, the water accumulation might be the main root cause of cell dying in this early stage of cell operation.

Figure 1. (a) Comparison of parallel and serpentine flow fields for CO2 electrolysis of 0.5Ni-SAC in a 100cm2 MEA electrolyzer under 200ml/min of CO2, 100ml/min 0.25M KOH, and IrO2-TiPt anode at 100mA/cm2 and (b) different conditions.

Dried -  200ml/minCO2, 0.25M KOH, 100mA/cm2

50mM CH3COOH Humidified - 200ml/minCO2, 0.25M CsOH, 100mA/cm2

- Upcoming tasks

  - Solutions for fully preventing liquid leakage: Optimizing gasket material/thickness and compression load

  - 100cm2 MEA electrolyzer – CO2 electrolysis of serpentine-BPM system under a humidified 1000ml/min CO2, 100ml/min of 0.25M KOH, and IrO2-TiPt anode at 100mA/cm2

  - 100cm2 MEA electrolyzer – CO2 electrolysis of serpentine-BPM system under a humidified 500ml/min CO2, 100ml/min of 0.25M KOH, and IrO2-TiPt anode at 100mA/cm2