Sothearoth Heng

NCR ID: 803198

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2023-20170-EN

December 2023

Project Title:

Development of Cu-based catalyst for electrochemical CO2 reduction to C2 products: combined computational chemistry and electrochemical engineering approach

Checked by:

...........................................................

Dr. Pongkarn Chakthranont

December monthly report

- Tasks list for December

- Literature Review on synthesis of Ag NPs and NH2-Ag NPs through different methods

- Experimental design, synthesis, and characterization of silver nanoparticles

- Investigation of CO2RR performance in a zero-gap electrolyzer using different types of membrane (Bipolar, Fumasep AEM, and Sustainion AEM)

- Investigation of CO2RR performance in a zero-gap electrolyzer using a sputtered Ag cathode electrode

- Experimental

Synthesis of Ag NPs via chemical reduction method

Briefly, 3.82 g of AgNO3 precursor was thoroughly dissolved in 300 ml of DI water to make 75mM AgNO3 solution. NaBH4 was used as a reducing agent. 0.94 g of NaBH4 was carefully dissolved in 300 ml of cold DI water under 0C ice bath and stirring rate of 500 rpm. Afterwards, the AgNO3 solution was slowly dropped into NaBH4 with a flow rate of 10 ml/min, and then a transparent solution turned into black color, indicating the formation of Ag NPs. After completely adding AgNO3 solution, the mixture solution was further stirred at 500rpm for another hour to complete the reaction. The precipitated Ag product was filtrated and washed by DI and EtOH for several time and followed by drying under 60C for 6h. The obtained Ag NPs was further characterized by FESEM.

Synthesis of NH2-Ag NPs

The amino functionalized silver nanoparticles catalyst (NH2-Ag NPs) was prepared by a hydrothermal method.18 Initially, 16.4 mg of NaCl and 1.34 PVP (MW = 55000) were dissolved and vigorously stirred in 20 ml of ethylene glycol (EG) to make a transparent solution (denoted as solution A). 0.69 g of AgNO3 was dissolved in 10 ml of EG to make a silver solution, (denoted as solution B). 31.1 mg of butylamine (BNH2) was also dissolved in 10ml of EG to obtain a functionalized-ligand solution (denoted as solution C). Afterwards, solution B and C was slowly added to solution A under stirring. 8 ml of glycerol was then added into the above mixture solution to form a colloidal solution. Next, the colloidal solution was transferred to a 100 ml Teflon-lined stainless autoclave and heated in an oven at 160C for 2h. Finally, the precipitated NH2-Ag NPs product was centrifuged, washed with EtOH for several time, and overnight dried under 40C in vacuum oven. The obtained NH2-Ag NPs was further characterized FESEM.

Experiment conditions

30ml of 1M KOH anolyte was recirculated into the anodic compartment with a flow rate of 30rpm by a peristatic pump. The cathodic flow field was fed by 30 ml/min of a humidified pure CO2 under room temperature.

Study of different types of membranes: NiFe and commercial Ag were used as anode and cathode electrodes, while different membranes, such as fumasep Bipolar, AEM and Sustainion AEM were used in this section.

- Result

Characterization of as-prepared Ag NPs samples

As can be seen in Fig. 1, the size of Ag nanoparticles obtained from a chemical reduction method was approximately 900nm with a random particle size distribution. These results might be caused from rapid adding of AgNO3 solution into NaBH4 (10ml/min), unconcerned rising of ice bath temperature, and short reaction time.

Figure 1. FE-SEM of as-prepared Ag NPs

Based on FE-SEM images, impurities and different morphologies with cubic and rod shapes was observed in the as-prepared catalyst surface, which might result from short mixing time, reaction time, and centrifugation time. Therefore, increasing all these parameters would prolongate the particles to gently grow into a unique shape with less impurity rather than aggregating with a random morphology.

Figure 2. FE-SEM of as-prepared NH2-Ag NPs

440 nm of the sputtered Ag layer appearing above the carbon layer was obtained after sputtering for 15min.

Figure 3. FE-SEM side view image of a sputtered Ag.

The Ag layer of a commercial Ag as shown in Fig. 4 was approximately 6.4 µm.

Figure 4. FE-SEM side view image of a commercial Ag

Electrochemical CO2 reduction performance with different membranes

According to Fig. 5, a MEA cell configuration with a Bipolar membrane (BPM) showed high HER selectivity and FE(H2) of approx. 50-60%, and by replacing a bipolar membrane with sustainion AEM, the FE(CO) was highly increased to 65% with a very low competing reaction (HER). Similar results to our case were also encountered.12,13 In BPM-MEA system, the local pH of cathode compartment becomes more acidic due to high H+ ion concentration, which is not productive in the CO2RR performance, but highly productive in the HER, leading to HER dominates in the system.14,15 On the other hands, the AEM-MEA system highly performed CO2RR to CO product at 50 mA/cm2. However, the total faradaic efficiency was still less than 100%, and according to other reports, this could result from the formation of another byproduct, likely to be HCOO- besides CO and H2.16 Based on the aforementioned, AEM-MEA system seems to be more reasonable for electrochemical CO2RR in AEM-MEA system than BPM and Fumasep AEM (the results did not show due to it was impossible to operate) systems, even though there is a tradeoff regarding the CO2 crossover to anodic compartment (massive loss) during the operation.

Figure 5. Faradaic Efficiency of difference cell configurations under applied j of 50 mA/cm2

Electrochemical CO2 reduction performance with a sputtered Ag cathode

A CO2RR performance was conducted with a cell configuration as NiFe/AEMSust/Agsput under applied current density (j) range of 50-200 mA/cm2. The maximum FE(CO) was obtained under j of 100-150mA/cm2 with %FE(H2) approx. 8-12%, while the FE(CO) at the lowest (50 mA/cm2) and highest j (200 mA/cm2) was approx. 60-64%. These results showing that the sputtered Ag cathode catalyst with a Ag layer of 440 nm exhibited similar performance to the previous experiment with a commercial Ag cathode. In order to optimize the eCO2RR performance with the use of sputtered Ag cathode, the investigation of the sputtering time and thickness of Ag layer should also be address. Besides the what we have reported, we also observed the NiCO3 formation on the NiFe anode resulting from the interaction between crossover carbonate and bicarbonate ions and Ni ions, which subsequently caused the anode degradation and Ni poisoning on Ag layer.17 Therefore, either an alternative anode should be considered or replacing the KHCO3 anolyte with KOH solution at a high flow rate could mitigate a drop in anolyte pH.

Figure 6. Faradaic efficiency of eCO2RR performance with a sputtered Ag cathode under 50-200 mA/cm2

- Summary

In summary, Ag NPs and NH2-Ag NPs cathode catalysts were successfully prepared under chemical reduction and hydrothermal methods, respectively. A spherical Ag particle size was largely around 900 nm. NH2-Ag NPs exhibited uncertain morphologies (cubic and rod shape) along with impurities, thereby optimizing the synthesis parameters should be considered in the next batch. A sputtered Ag cathode with a Ag thickness of 440nm showed similar performance to commercial Ag cathode catalyst with a maximum FE(CO) of 74%. AEM-MEA system was the best systems for CO2RR to CO product with massive CO2 loss to the anode side, while BPM system struggling with the suppression of CO2RR under an acidic environment. Electrodes degradation by the formation of NiCO3 and Ni2+ crossover becomes a challenge problem in a zero-gap electrolyzer system, thus either alternative anodes or replacing the KHCO3 with KOH anolyte should be considered.

- Upcoming Tasks

- Synthesis of Ag-NPs and NH2-Ag NPs catalysts by controlling parameters

- Spray coating as-prepared catalysts on carbon paper for further use as cathode materials

- CO2RR performance test in a zero-gap electrolyzer with a cell configuration IrO2/AEMSustaionion/Ag or NiFe/AEMsustainion/Ag with KOH anolyte

- Reference

12. Kailun Yang, Mengran Li, Siddhartha Subramanian, Marijn A. Blommaert, Wilson A. Smith, and Thomas Burdyny. ACS Energy Letters 2021 6 (12), 4291-4298.

13. Colin P. O’Brien, Rui Kai Miao, Shijie Liu, Yi Xu, Geonhui Lee, Anthony Robb, Jianan Erick Huang, Ke Xie, Koen Bertens, Christine M. Gabardo, Jonathan P. Edwards, Cao-Thang Dinh, Edward H. Sargent, and David Sinton. ACS Energy Letters 2021 6 (8), 2952-2959

14. Li, Yuguang C.; Zhou, Dekai; Yan, Zhifei; Goncalves, Ricardo H.; Salvatore, Danielle A.; Berlinguette, Curtis P.; Mallouk, Thomas E. ACS Energy Letters (2016), 1 (6), 1149-1153

15. Danielle A. Salvatore, David M. Weekes, Jingfu He, Kevan E. Dettelbach, Yuguang C. Li, Thomas E. Mallouk, and Curtis P. Berlinguette. ACS Energy Letters 2018 3 (1), 149-154

16. Gastón O. Larrazábal, Patrick Strøm-Hansen, Jens P. Heli, Kevin Zeiter, Kasper T. Therkildsen, Ib Chorkendorff, and Brian Seger. ACS Applied Materials & Interfaces 2019 11 (44), 41281-41288

17. Ádám Vass, Balázs Endrődi, Gergely Ferenc Samu, Ádám Balog, Attila Kormányos, Serhiy Cherevko, and Csaba Janáky. ACS Energy Letters 2021 6 (11), 3801-3808

18. Liu, Z., Yan, T., Shi, H., Pan, H., & Kang, P. (2024). Grafting amine-functionalized ligand layer on catalyst for electrochemical CO2 capture and utilization. Applied Catalysis B: Environmental, 343, 123456.