……..........................................................

Dr. Pongkarn Chakthranont

Sothearoth Heng

NCR ID: 803198

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2023-20170-EN

March 2024

Project Title:

Development of Cu-based catalyst for electrochemical CO2 reduction to C2 products: combined computational chemistry and electrochemical engineering approach

March monthly report

- Tasks list for March

- Investigation of eCO2RR performance under higher CO2 flow rate (100-200ml/min) using sputtered Ag cathode

- Screening the eCO2RR performance of different single-atom catalysts (Co, Cu, Fe, Zn, and Ni-2D-NOC) under CO2 gas stream of 150ml/min and j of 200mA/cm2

- Synthesis of Ni-2D-NOC catalyst via pyrolysis method under Argon gas.

- Studies of influence of varied cathodic gas feed compositions on CO selectivity:

  - Absolute CO2 supply (15, 30, 100, 150 ml/min)

  - Gas mixture of 15%CO2/85%N2 (total flow rate of 100ml/min)

  - Gas mixture of 95%CO2/5%O2 (total flow rate of 100ml/min)

- Experimental Procedure

Synthesis of Ni-2D-NOC catalyst via pyrolysis method

The synthesis of Ni-2D-NOC catalyst was completely followed the previous report.1 Initially, Ni-Phc, Urea, and Dicy (weight ratio of 1:5:5) were ground-mixed thoroughly together. Then, the mixture was placed in a quartz boat that was closed with a lid and pyrolyzed at 800 °C (ramp rate = 10 °C·min–1) in a tube furnace under an Ar atmosphere (flow rate = 200 sccm) for 2h.

Preparation of Ni-2D-NOC cathode electrodes via spray coating method

The as-prepared Ni-2D-NOC catalyst was spray-coated onto Sigracet 36BB carbon paper. Briefly, 50 mg of the Ni-2D-NOC and 127µL or 10% by catalyst weight of XA-9 Binder were ultrasonically mixed with IPA for 30 min to form a dark colloidal solution which then was sprayed onto carbon paper with 0.5 ml/min on 95 C hotplate to obtain ~ 0.5  0.15 mg/cm2.

Electrochemical CO2RR measurements

A 5 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The Ni foam, AEM (X37-50 Grade RT, Dioxide Materials), and sputtered Ag and M-2D-NOC (M denoted as Co, Cu, Fe, Zn, and Ni) cathode catalysts were employed as the anode, membrane, and cathode electrode, respectively. 50 ml of 0.5M KOH was recirculated and used throughout the experiment as the anolyte at 8 ml/min. Different humidified gas feed compositions was introduced into the cathodic inlet under various flow rates. The cathodic outlet was directly injected into an online gas-chromatography for further gas products analysis.

- Results

Influence of CO2 flow rate on eCO2RR performance of sputtered Ag cathode

In the previous report, we had conducted CO2RR at 5-50 mlCO2/min and proved that the FE(CO) was CO2 flow rate dependent with a maximum FE(CO) of 76% at 30 mlCO2/min. To further extend the understanding of the influence of higher absolute CO2 amounts, the CO2RR performance of the sputtered Ag was conducted at 100-200 mlCO2/min. As shown in Fig. 1, we observed a slight raise in FE(CO) with approx. 5% of FE(H2) at 100 mlCO2/min comparing to 30 mlCO2/min. By further elevating the CO2 flow rate to 150 mlCO2/min, the CO selectivity was drastically boosted in terms of achieving higher FE(CO) of approx. 89% with 5% FE(H2), and reaching the equilibrium at 200 mlCO2/min. These results demonstrated that the decreased kinetic of CO2RR at lower CO2 supply might be attributed to the CO2 deficiency on the catalytic active site of Ag which can be solved by increasing the CO2 flow rate.2

Figure 1. Faradaic efficiency of the MEA electrolyzer with sputtered Ag cathode under CO2 flow rate range of 5-200 ml/min at 200mA/cm2.

Influence of different cathodic gas feed compositions on CO selectivity of Ni-2D-NOC cathode catalyst

The CO2RR was performed at various absolute CO2 flow rate (15, 30, 100, and 150 ml/min), j of 200mA/cm2, and 0.5M KOH anolyte flow rate of 8 ml/min to identify the effect of CO2 supply on overall MEA performance. A similar trend of poor CO selectivity to sputtered Ag was also noticed in Ni-2D-NOC cathode catalyst in which the current densities of both sputtered Ag and Ni-2D-NOC cathodes, whose FE(H2) drastically increased at low-CO2 supply, were strongly influenced by a competitive HER on the active sites due to the scarcity of surface-adsorbed CO2. By further raising the amount of CO2 from 15 to 30, 100, and 150 ml/min, the FE(CO) was exponentially increased with a maximum FE(CO) of approx. 98% at CO2 supply of 150 ml/min, suggesting that the CO2 to CO performance of Ni-2D-NOC catalyst was prone to correlating with the amount of CO2. On the other hand, the direct conversion of low concentrated CO2 feed is crucial for practical application with a direct flue gas that mainly contains of 5-40% CO2 balanced by N2 with trace amount of O2 as the feedstock. (18 in low C). Diluted 15% CO2/N2 and 95%CO2/5%O2 gas mixtures were used as cathodic gas feed to determine the effect of low-concentrated CO2 feed or low-PCO2 (CO2 partial pressure) and competitiveness of oxygen reduction reaction (ORR) on CO selectivity of the MEA electrolyzer, respectively. As can be seen in Fig. 2, for a 15%CO2/N2 gas feed, the CO selectivity exhibited a similar trend with absolute CO2 flow rate of 15 ml/min but even poorer CO2RR performance due to lower CO2 concentration could lead to higher competing HER on the catalytic active sites (extrinsic factors, such as anolyte flow rate or water crossover management might play an essential role to suppress HER activity at low-PCO2).3–5 The oxygen reduction reaction (ORR) is a known catalytic reaction that can occur under reducing potentials and is thermodynamically more favorable than CO2RR to CO.6 In the presence of 5%O2 in 95%CO2 cathodic gas feed, CO2RR performance and total faradaic efficiency were significantly detrimental by ORR activity. The CO selectivity was completely fell off after 1h of operating duration, suggested that high water content produced by ORR activity at the cathode surface could possibly enhance a competing HER activity and cause GDE flooding.

Figure 2. Faradaic Efficiency of MEA electrolyzer with Ni-2D-NOC cathode under 200mA/cm2 and different cathodic gas compositions (15-150 mlCO2/min, 15%CO2/N2, and 95%CO2/O2).

CO2RR performance of different cathode materials

The CO2RR performance of different Ag-based catalysts and M-2D-NOC single atom catalysts was prescreened under 200mA/cm2 and 150mlCO2/min. As shown in Fig. 3, Ag-based cathode catalysts exhibited a high CO selectivity in terms of achieving a maximum FE(CO) of approx. 89% with a slight H2 byproduct. Meanwhile, most of as-prepared and exfoliated-M-2D NOC single atom catalysts (M = Co, Zn, Ni, Fe, and Cu), except the as-prepared Ni-2D-NOC, strongly suffered from the GDE flooding due to their high hydrophilicity, proton affinity, and catalytic HER which could lead to suppress CO2RR performance. On the other hands, the catalytic performance of Ni-2D-NOC seems unaffected by HER, showing superior CO2 to CO activity compared to other materials, with a maximum FE(CO) of approx. 98%.

Figure 3. Faradaic efficiency of different cathode materials under applied current density of 200mA/cm2 and 150 mlCO2/min.

- Summary

In summary, both sputtered Ag and Ni-2D-NOC cathode catalysts showed improved CO2RR performance when the absolute amount of CO2 was increased. However, the Ni-2D-NOC exhibited poor CO2 to CO activity at low absolute amounts of CO2 and in a 15% CO2/N2 gas mixture due to a lack of surface-adsorbed CO2 and competitive HER on the catalytic active sites. The addition of 5% O2 in a 95% CO2 gas feed caused severe CO2RR suppression but facilitated ORR activity due to its thermodynamic favorability. Evaluation of the CO2RR performance of M-2D-NOC single atom catalysts revealed that the as-prepared Ni-2D-NOC catalyst outperformed others in terms of high CO2 to CO activity with a maximum FE(CO) of approx. 98%.

- Upcoming tasks

- Synthesis of Ni2-2D-NOC with a Ni-phc:Urea:Dicy ratio of 2:5:5

- CO2RR performance measurement of as-prepared Ni2-2D-NOC

- Investigation of CO2RR performance of Ni-2D-NOC with different mass loading (0.65, 1, and 1.5 mg/cm2)

- Literature review on Ni single atom catalysts for electrochemical reduction of CO2 to CO

- References

1.	Butburee, T. et al. General Pyrolysis for High-Loading Transition Metal Single Atoms on 2D-Nitro-Oxygeneous Carbon as Efficient ORR Electrocatalysts. ACS Appl Mater Interfaces (2024)

2.	Kim, D. et al. Electrocatalytic Reduction of Low Concentrations of CO2Gas in a Membrane Electrode Assembly Electrolyzer. ACS Energy Lett 6, 3488–3495 (2021).

3.	Salvatore, D. A. et al. Designing anion exchange membranes for CO2 electrolysers. Nature Energy 2021 6:4 6, 339–348 (2021).

4.	Wheeler, D. G. et al. Quantification of water transport in a CO2 electrolyzer. Energy Environ Sci 13, 5126–5134 (2020).

5.	Weng, L. C., Bell, A. T. & Weber, A. Z. Towards membrane-electrode assembly systems for CO2 reduction: a modeling study. Energy Environ Sci 12, 1950–1968 (2019).

6.	Ge, X. et al. Oxygen Reduction in Alkaline Media: From Mechanisms to Recent Advances of Catalysts. ACS Catal 5, 4643–4667 (2015).