……....................................

Dr. Pongkarn Chakthranont

Project:

Advancing Integrated Materials and Devices for Electrochemical CO2 Reduction (AIM-COR)

Sothearoth Heng (ID: 803198)

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2026-25421-EN

June 2026 report

June monthly report

- To-do list in June

- 100cm2 MEA electrolyzer – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 800ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2

- 100cm2 MEA electrolyzer operation in 30 position – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 400ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2

- Experimental Procedure

Synthesis of 0.5NiSAC by pyrolysis method

The synthesis of 0.5NiSAC catalyst was followed by our previous work. Initially, nickel phthalocyanine (NiPc), urea, and dicyanamide precursors were stoichiometrically weighed according to mass ratios of 0.5:5:5. Subsequently, the mixture was thoroughly mixed and ground until a homogeneous midnight blue powder was obtained. The fine powder was then transferred into a quartz boat covered with a capsule lid and subjected to polymerization at 800 - 900 °C (ramp rate = 10 °C·min⁻¹) in a horizontal tube furnace under an argon atmosphere (flow rate > 200 sccm) 2 - 4 h.

Preparation of AgNPs cathode via spray coating method

The NiSAC gas-diffusion electrode was fabricated by spray coating onto Sigracet 39BB carbon paper or hydrophilic carbon cloth substrates. Typically, 150 mg of AgNPs and 381 μL of XC-2 ionomer were ultrasonically dispersed in 10 mL of isopropanol (IPA) for at least 1 h to form a homogeneous dark colloidal suspension. The ink suspension was subsequently spray-coated onto a 12 x 12 cm2 carbon substrate using an automated, custom-built spraying setup equipped with a syringe pump operating at a flow rate of 0.6 mL min⁻1 on a hotplate maintained at 130°C, yielding a catalyst mass loading of 0.5 ± 0.1 mg.cm⁻2 AgNPs.

Electrochemical measurements in membrane-electrode assembly (MEA) electrolyzer

5 and 100cm2 MEA electrolyzer operational set-up

A 100 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The IrO2-TiPt felt (10.5 x 10.5 cm2), AEM (12 x 12 cm2), and AgNPs (10.5 x 10.5 cm2) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled with 0.25µm PTFE gasket and tightened at a compression force of 8 ft.lb. 10 L of 0.1 M KHCO3 was recirculated and used throughout the experiment as the anolyte at 100 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 200-800 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Effect of CO₂ flow rate on FE(CO) durability in the 100 cm² parallel flow-field

To evaluate the effect of CO₂ flow rate on operational durability, the 100 cm² parallel flow-field MEA was operated galvanostatically at 100 mA·cm⁻² under humidified CO₂ (50 mM CH₃COOH) supplied at 200, 400, and 800 ml·min⁻¹ (2, 4, and 8 ml·min⁻¹·cm⁻², respectively). As shown in Figure 1, all three conditions delivered a comparable initial FE(CO) of ~90–95 %, whereas the duration of stable operation scaled monotonically with the CO₂ flow rate: the 200 ml·min⁻¹ condition declined first (~20 h), followed by 400 ml·min⁻¹ (~25 h), while 800 ml·min⁻¹ sustained FE(CO) the longest (~33–36 h, FE(CO) ~78–80 % at ~33 h). Throughout each run, the cell voltage remained stable at ~3.2–3.3 V. The stable voltage signature indicates that failure proceeded by surface channel water blockage rather than deep gas-diffusion-electrode pore flooding, for which a decreasing voltage would be expected; the PTFE hydrophobicity of the GDE was therefore retained. The improvement with increasing flow rate is attributed to the higher per-channel gas velocity, which clears accumulated liquid water more effectively and delays channel blockage. According to our previous results, increasing the CO₂ flow rate delays but does not eliminate parallel-flow-field failure, since the underlying low per-channel velocity at any individual channel remains the geometric constraint. The complementary cell-voltage and cathode vent-pressure profiles for the 800 ml·min⁻¹ condition (Figure 1, lower panels) confirm stable operation: the second run maintained ~3.2 V for ~40 h with pressure excursions limited to gas-chromatography injection events, whereas the first run exhibited an abrupt voltage drop at ~13–15 h consistent with a short-circuit event rather than a flow-field limitation. It is worth noting that this short-circuit behaviour is distinct from the gradual flow-field decline and is addressed separately below.

Figure 1. Influence of CO₂ flow rate (200, 400, 800 ml·min⁻¹) on FE(CO) and cell voltage of the AgNPs (50 nm, ~0.6 mg·cm⁻²) / AEM / IrO₂-TiPt 100 cm² parallel-flow-field MEA under 50 mM CH₃COOH humidified CO₂, 150 ml·min⁻¹ 0.1 M KHCO₃ anolyte, 100 mA·cm⁻². Lower panels: cell-voltage and cathode vent-pressure profiles for two 800 ml·min⁻¹ runs with a PiperION AEM.

Effect of membrane thickness on short-circuit susceptibility under 30° tilted operation

To ascertain the effect of membrane thickness on operational stability during gravity-assisted drainage, the 100 cm² parallel flow-field MEA was tilted to a 30° orientation and operated at 100 mA·cm⁻² under 400 ml·min⁻¹ humidified CO₂, comparing a thin 20 µm PiperION membrane (Figure 2) with a thicker 40 µm AEM (Figure 3); the flat 0° orientation was run in parallel as a reference in both cases. As shown in Figure 2, the 20 µm membrane delivered a high initial FE(CO) of ~96–98 % that remained stable to ~10 h, after which a first short-circuit event (~10 h) reduced FE(CO) by ~20 %, followed by a second short-circuit event (~25 h) that reduced FE(CO) by a further ~35 %. The mean cell voltage was 3.227 ± 0.072 V, remaining otherwise flat between events with discrete downward steps coinciding with each short-circuit. This signature — an abrupt voltage perturbation and a stepwise FE(CO) loss against an otherwise stable baseline — identifies an electrical breach of the membrane rather than GDE flooding or kinetic degradation. In contrast, the 40 µm membrane (Figure 3) sustained ~95 % FE(CO) without any short-circuit event over a markedly longer run. This comparison demonstrates that membrane thickness governs short-circuit susceptibility under the mechanical loading of the tilted 100 cm² assembly: the 20 µm membrane is too thin to withstand compression in the tilted configuration, whereas the 40 µm membrane preserves electrical isolation. It is worth noting that the 30° tilt alone is insufficient to prevent failure when the membrane is thin, so adequate membrane thickness is a prerequisite for exploiting tilted-drainage operation.

Figure 2. Long-term CO₂ electrolysis of the AgNPs (50 nm, ~0.6 mg·cm⁻²) / PiperION 20 µm / IrO₂-TiPt 100 cm² parallel-flow-field MEA at 0° and 30° orientation under 50 mM CH₃COOH humidified CO₂ (400 ml·min⁻¹), 100 ml·min⁻¹ 0.1 M KHCO₃, 100 mA·cm⁻². Lower panel: cell voltage (3.227 ± 0.072 V) and cathode outlet pressure, with two short-circuit events annotated.

Recovery interventions and post-mortem analysis of extended 100 cm² operation

To evaluate whether in-situ recovery interventions can extend operation in the tilted configuration, the 40 µm AEM cell at 30° orientation (400 ml·min⁻¹ humidified CO₂, 100 mA·cm⁻²) was operated with periodic maintenance and subsequently disassembled for post-mortem inspection. As shown in Figure 3, the cell sustained ~95 % FE(CO) at a stable cell voltage of ~3.2–3.3 V for ~195–200 h, with the cathode outlet pressure held at ~30–40 mBar. Four interventions were applied over the run: an immediate shutdown-and-rerun at 80 h, a 4 h dried-N₂ purge with rerun at 87 h, an 8 h dried-N₂ purge at 140 h, and a refresh of the 0.1 M KHCO₃ anolyte at 160 h. The transient FE(CO) excursions to ~80 % around 80, 110, and 150 h, each recovering after the corresponding intervention, indicate that the dominant degradation was reversible channel water/salt accumulation rather than irreversible catalyst or membrane failure; the stable voltage throughout confirms the channel-blockage regime, and the dried-N₂ purge re-opened the gas pathways while the anolyte refresh restored the K⁺/carbonate balance. Post-mortem inspection of the disassembled cell (Figure 4) showed relatively clean parallel-flow-field channels with only minor residue, mild grayish salt deposition on the AgNPs gas-diffusion electrode, and an intact 40 µm membrane with no visible physical breach, all consistent with the sustained FE(CO) and stable voltage recorded during the run. These observations indicate that combining a 40 µm membrane, 30° gravity-assisted drainage, and periodic dried-N₂ purging with anolyte refresh extends stable 100 cm² operation to ~195–200 h, with mild GDE salt deposition remaining the residual degradation pathway to be addressed.

Figure 3. Long-term CO₂ electrolysis of the AgNPs (50 nm, ~0.6 mg·cm⁻²) / AEM 40 µm / IrO₂-TiPt 100 cm² parallel-flow-field MEA at 0° and 30° orientation under 50 mM CH₃COOH humidified CO₂ (400 ml·min⁻¹), 100 ml·min⁻¹ 0.1 M KHCO₃, 100 mA·cm⁻², reaching ~195–200 h. Lower panel: cell voltage and cathode outlet pressure with recovery interventions annotated (shutdown-rerun at 80 h; dried-N₂ purge at 87 h and 140 h; anolyte refresh at 160 h).

Figure 4. Post-mortem photographs of the 100 cm² MEA after 195 h of CO₂RR, showing the parallel flow-field plate, AgNPs gas-diffusion electrode, and 40 µm AEM after 140 h and 195 h of operation.

Upcoming tasks

- 100cm2 MEA electrolyzer – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 800ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2

- 100cm2 MEA electrolyzer operation in 45 position – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 400 or 800 ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2