……....................................

Dr. Pongkarn Chakthranont

Project:

Advancing Integrated Materials and Devices for Electrochemical CO2 Reduction (AIM-COR)

Sothearoth Heng (ID: 803198)

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2026-25421-EN

August 2026 report

August monthly report

- To-do list in August

- 100cm2 MEA electrolyzer operation in 15 and 45 position – CO2 electrolysis of 0.5NiSAC (850C-4h-10 C.min-1) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 400 ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 200mA/cm2

- Fabrication of IrO2-TiPt electrode and OER performance evaluation

- 5cm2 MEA electrolyzer – Long-term CO2 stability of 0.5Ni-SAC (850C-4h-10 C.min-1) catalyst in AEM system at 100mA/cm2

- Experimental Procedure

Synthesis of 0.5NiSAC by pyrolysis method

The synthesis of 0.5NiSAC catalyst was followed by our previous work. Initially, nickel phthalocyanine (NiPc), urea, and dicyanamide precursors were stoichiometrically weighed according to mass ratios of 0.5:5:5. Subsequently, the mixture was thoroughly mixed and ground until a homogeneous midnight blue powder was obtained. The fine powder was then transferred into a quartz boat covered with a capsule lid and subjected to polymerization at 800 - 900 °C (ramp rate = 10 °C·min-1) in a horizontal tube furnace under an argon atmosphere (flow rate > 200 sccm) 2 - 4 h.

Preparation of AgNPs cathode via spray coating method

The NiSAC gas-diffusion electrode was fabricated by spray coating onto Sigracet 39BB carbon paper or hydrophilic carbon cloth substrates. Typically, 150 mg of AgNPs and 381 μL of XC-2 ionomer were ultrasonically dispersed in 10 mL of isopropanol (IPA) for at least 1 h to form a homogeneous dark colloidal suspension. The ink suspension was subsequently spray-coated onto a 12 x 12 cm2 carbon substrate using an automated, custom-built spraying setup equipped with a syringe pump operating at a flow rate of 0.6 mL min-1 on a hotplate maintained at 130°C, yielding a catalyst mass loading of 0.5 ± 0.1 mg.cm-2 AgNPs.

Electrochemical measurements in membrane-electrode assembly (MEA) electrolyzer

5 and 100cm2 MEA electrolyzer operational set-up

A 100 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The IrO2-TiPt felt (10.5 x 10.5 cm2), AEM (12 x 12 cm2), and AgNPs (10.5 x 10.5 cm2) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled with 0.25µm PTFE gasket and tightened at a compression force of 8 ft.lb. 10 L of 0.1 M KHCO3 was recirculated and used throughout the experiment as the anolyte at 100 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 200-800 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Effect of cell tilt angle on CO₂RR durability at 100 cm² and 200 mA cm⁻²

To evaluate the effect of gravity-assisted drainage on flooding-limited durability, the 100 cm² 0.5NiSAC/AEM cell equipped with a parallel cathode flow-field was operated at 200 mA cm⁻² while tilted 15° and 45° from vertical, with 50 mM CH₃COOH-humidified CO₂ supplied at 400 mL/min and 100 mL/min of 0.1 M KHCO₃ recirculated as the anolyte. As shown in Figure 1, FE(CO) was maintained at ≈ 97 % for both tilt angles over the majority of each run, while the cell voltage rose gradually from ≈ 3.15 V to ≈ 3.7 V for the 15° configuration, which reached ≈ 72 h before failure. In contrast, the 45° configuration failed earlier at ≈ 60 h, where the cell voltage underwent a sharp oscillatory excursion to ≈ 4.3 V at ≈ 58 h accompanied by the complete GDE flooding event annotated on the outlet-gas channel, in which the cathode outlet flow spiked from ≈ 0.30 to ≈ 0.45 SLPM. The oscillatory voltage signature and the concurrent outlet-flow surge are consistent with accumulated liquid water breaching the gas pathway and flooding the gas-diffusion electrode, rather than a kinetic or membrane failure. That the shallower 15° tilt outlasted the steeper 45° tilt indicates that, at 200 mA cm⁻², the higher water-generation rate overwhelms the incremental drainage benefit of a steeper angle, so the deeper tilt does not translate into longer flooding-limited durability. It is worth noting that the periodic pressure spikes at ≈ 4, 27, and 67 h (15°) and ≈ 4, 16, and 44 h (45°) correspond to the in-situ recovery interventions; the reversibility of these excursions supports channel/GDE water management, not irreversible degradation, as the limiting mechanism.

Figure 1. Long-term CO₂ electrolysis of the 100 cm² 0.5NiSAC | AEM (40 µm) | IrO₂-TiPt MEA under 15° and 45° tilted operation at 200 mA cm⁻², with 50 mM CH₃COOH-humidified CO₂ (400 mL/min), 100 mL/min of 0.1 M KHCO₃ anolyte, 350/250 µm silicone gaskets, and 8 ft·lb compression: (top) %FE(CO) and cell voltage versus time for both tilt angles; (bottom) per-angle pressure profiles (anode/cathode inlet and outlet) and outlet-gas flow profiles.

Reproducibility and voltage improvement of the re-fabricated IrO₂-TiPt anode

To ascertain the reproducibility of the re-fabricated anode and its effect on cell voltage, the OER performance of the as-prepared IrO₂/TiPt-felt electrodes was benchmarked at 100 cm² and 100 mA cm⁻² under a humidified N₂ feed (200 mL/min) with 100 mL/min of 0.1 M KHCO₃ anolyte, such that the measured cell voltage isolates the anodic contribution in the absence of CO₂RR. As shown in Figure 2, the two re-fabricated anodes (New-IrO₂-1 and New-IrO₂-2) sustained a stable cell voltage of ≈ 4.5–4.55 V and near-overlapping traces over the 1 h test, whereas the previous batch (Old-IrO₂) operated at ≈ 4.8 V. The ≈ 0.3 V reduction in cell voltage demonstrates that the revised fabrication yields a more active anode, while the close overlap of the two new electrodes confirms batch-to-batch reproducibility of the thermal-deposition procedure. This improvement directly lowers the operating voltage of the full CO₂RR cell and provides a qualified anode for the subsequent long-term stability tests.

Figure 2. OER performance of as-prepared IrO₂/TiPt-felt anodes (Old-IrO₂, New-IrO₂-1, New-IrO₂-2) in a 100 cm² MEA (39BB-GDE | BPM | IrO₂-TiPt) under humidified N₂ (200 mL/min) with 100 mL/min of 0.1 M KHCO₃ anolyte at 100 mA cm⁻²: cell voltage versus time.

Effect of cell active area (5 vs 100 cm²) on long-term CO₂RR stability at 100 mA cm⁻²

To evaluate the effect of cell active area on long-term durability, the 0.5NiSAC (850 °C-4h-10 °C min⁻¹) | AEM (40 µm) | IrO₂-TiPt system was operated at 100 mA cm⁻² in both 5 cm² and 100 cm² MEA cells under CH₃COOH-humidified CO₂ (4 mL CO₂ min⁻¹ cm⁻²) with 100 mL/min of 0.1 M KHCO₃ anolyte and periodic anolyte refreshes. As shown in Figure 3, both cells sustained FE(CO) of ≈ 97–98 % and a cell voltage of ≈ 3.2 V and tracked one another closely through ≈ 520 h, with the 5 cm² cell exhibiting low per-segment degradation rates of 0.450–1.174 mV h⁻¹ across its ≈ 595 h run. Beyond ≈ 520 h, however, the 100 cm² cell entered an accelerated degradation regime, with the final-segment rate rising to 4.512 mV h⁻¹ — roughly five- to seven-fold higher than its earlier segments (0.652–0.830 mV h⁻¹) — followed by a sharp voltage rise and an FE(CO) collapse to ≈ 70 % near 590 h. The sawtooth voltage recoveries after each anolyte refresh confirm that the baseline degradation is dominated by reversible K⁺/carbonate accumulation, whereas the terminal runaway unique to the larger cell indicates a scale-dependent onset of irreversible GDE-level salt/water accumulation. This scale-up penalty — comparable early-life behaviour but earlier terminal failure at 100 cm² — identifies late-stage salt/water management as the key barrier to translating small-cell stability to the 100 cm² scale.

Figure 3. Comparison of long-term CO₂ electrolysis stability of 5 cm² and 100 cm² 0.5NiSAC (850 °C-4h-10 °C min⁻¹) | AEM (40 µm) | IrO₂-TiPt MEA cells at 100 mA cm⁻² under CH₃COOH-humidified CO₂ (4 mL CO₂ min⁻¹ cm⁻²) with 100 mL/min of 0.1 M KHCO₃ anolyte: %FE(CO) and cell voltage versus time for (top) the 5 cm² cell, (middle) the 100 cm² cell, and (bottom) the overlaid comparison, with per-segment voltage degradation rates annotated between anolyte refreshes.

Upcoming tasks

- 100cm2 MEA electrolyzer operation in 15 position – CO2 electrolysis of 0.5NiSAC (850C-4h-10 C.min-1) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 400 ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 200mA/cm2

- 5cm2 MEA electrolyzer. – CO2 electrolysis of 0.5NiSAC (850C-4h-10 C.min-1) in AEM system at 250mA/cm2: Exploring the possible operational conditions (Effect of CO2 flow rate and acetic acid concentration)