……....................................

Dr. Pongkarn Chakthranont

Project:

Advancing Integrated Materials and Devices for Electrochemical CO2 Reduction (AIM-COR)

Sothearoth Heng (ID: 803198)

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2026-25421-EN

July 2026 report

July monthly report

- To-do list in July

- 100 cm2 MEA electrolyzer operation in 15° tilted position – CO2 electrolysis of 0.5NiSAC (850 °C-4h-10 °C·min−1) catalyst in AEM system with 350 µm / 250 µm silicone gaskets and 10 ft·lb under 50 mM CH3COOH humidified 400 mL/min CO2, 100 mL/min of 0.1 M KHCO3, and IrO2-TiPt anode at 100 mA/cm2 — long-term durability

- Exploring the possible high current density operation in 5cm2 AEM electrolyzer: CO2 electrolysis at current density range of 100 – 300 mA/cm2 and long-term stability test

- Experimental Procedure

Synthesis of 0.5NiSAC by pyrolysis method

The synthesis of 0.5NiSAC catalyst was followed by our previous work. Initially, nickel phthalocyanine (NiPc), urea, and dicyanamide precursors were stoichiometrically weighed according to mass ratios of 0.5:5:5. Subsequently, the mixture was thoroughly mixed and ground until a homogeneous midnight blue powder was obtained. The fine powder was then transferred into a quartz boat covered with a capsule lid and subjected to polymerization at 800 - 900 °C (ramp rate = 10 °C·min-1) in a horizontal tube furnace under an argon atmosphere (flow rate > 200 sccm) 2 - 4 h.

Preparation of AgNPs cathode via spray coating method

The NiSAC gas-diffusion electrode was fabricated by spray coating onto Sigracet 39BB carbon paper or hydrophilic carbon cloth substrates. Typically, 150 mg of AgNPs and 381 μL of XC-2 ionomer were ultrasonically dispersed in 10 mL of isopropanol (IPA) for at least 1 h to form a homogeneous dark colloidal suspension. The ink suspension was subsequently spray-coated onto a 12 x 12 cm2 carbon substrate using an automated, custom-built spraying setup equipped with a syringe pump operating at a flow rate of 0.6 mL min-1 on a hotplate maintained at 130°C, yielding a catalyst mass loading of 0.5 ± 0.1 mg.cm-2 AgNPs.

Electrochemical measurements in membrane-electrode assembly (MEA) electrolyzer

5 and 100cm2 MEA electrolyzer operational set-up

A 100 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The IrO2-TiPt felt (10.5 x 10.5 cm2), AEM (12 x 12 cm2), and AgNPs (10.5 x 10.5 cm2) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled with 0.25µm PTFE gasket and tightened at a compression force of 8 ft.lb. 10 L of 0.1 M KHCO3 was recirculated and used throughout the experiment as the anolyte at 100 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 200-800 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Effect of MEA tilt angle on long-term FE(CO) durability at 100 cm2

To evaluate the effect of MEA tilt angle on the long-term operational durability of the 0.5NiSAC catalyst, the 100 cm2 cell was operated galvanostatically at 100 mA·cm−2 (50 mM CH3COOH humidified CO2, 100 mL·min−1 of 0.1 M KHCO3) in a 0° (vertical) and a 15° tilted configuration. As shown in Figure 1, tilting the MEA cell from 0° to 15° markedly extended the stable FE(CO) operation from ~20 h to ~590 h, with FE(CO) maintained at ~95–100 % and the cell voltage held at ~3.0–3.2 V throughout the tilted run, while the single-pass CO2 utilisation stabilised at ~18–20 %. This pronounced improvement is attributed to the more effective gravity-assisted drainage of liquid water achieved under 15° tilted operation, which mitigates water accumulation within the gas-diffusion electrode (GDE) — one of the main causes of rapid cell failure in the vertical configuration. Near ~590 h, a gradual rise in cell voltage toward ~4 V was observed, accompanied by an increase in the CA-outlet gas signal and in parasitic HER activity, indicating the eventual onset of GDE flooding as accumulated water progressively restored the HER pathway at the expense of CO2 reduction. Post-mortem inspection of the disassembled cell (Figure 2) revealed no precipitated salt within the flow-field channels, confirming that carbonate/bicarbonate salt precipitation was not the primary cause of cell failure in this case and corroborating water-driven GDE flooding as the limiting degradation mechanism. Overall, the ~590 h of stable ~95–100 % FE(CO) represents the longest continuous 100 cm2 operation achieved to date and demonstrates that a modest 15° tilt substantially enhances the water management and durability of the 0.5NiSAC/AEM system.

Figure 1. Long-term CO2 electrolysis of the 0.5NiSAC (850 °C, 4 h, 10 °C·min−1) / AEM 40 µm / IrO2-TiPt 100 cm2 MEA at 15° tilt, showing FE(CO) and SPU (0° single-serpentine, 200 mL·min−1 vs 15° parallel, 400 mL·min−1), cell voltage, CA-outlet pressure, cell temperature, and outlet-gas concentration versus operational time under 50 mM CH3COOH humidified CO2, 100 mL·min−1 of 0.1 M KHCO3, at 100 mA·cm−2.

Figure 2. Post-mortem disassembly of the 100 cm2 MEA after 600 h of CO2 electrolysis, showing the cathode flow-field plate, the 0.5NiSAC gas-diffusion electrode (front and back), the AEM membrane, and the anode flow-field plate and housing.

Exploring the possible high current density operation in 5cm2 AEM electrolyzer

The 5 cm2 MEA cell (0.5NiSAC cathode, IrO2-TiPt anode) was revisited and operated at high current density range of 100–300 mA·cm−2 for 1 h at each current density on a Sustainion AEM (0.5 M CH3COOH humidified CO2 at 20 mL·min−1, 4 mL·min−1 of 0.1 M KHCO3). As shown in Figure 3, FE(CO) remained above 95 % from 100 to 250 mA·cm−2, with the single-pass CO2 utilisation rising to a maximum of 46.14 % at 250 mA·cm−2 (cell potential 2.94–3.28 V). Increasing the current density further to 300 mA·cm−2 lowered FE(CO) to 86.94 % while the SPU increased only marginally to 48.75 %, indicating that the reaction had entered a mass-transport-limited regime under the high-SPU, CO2-depleted condition.

To evaluate the consequences of operating in this depleted-CO2 zone, long-term stability tests were subsequently conducted on a PiperION AEM (40 µm). At 300 mA·cm−2, FE(CO) declined rapidly from ~85 % to ~65 % within only ~7 h of operation, consistent with the dominance of the competing HER. At 250 mA·cm−2, the cell sustained FE(CO) > 90 % for ~12 h before (bi)carbonate salt clogging of the flow-field channels caused cell failure; notably, raising the humidifier concentration from 0.5 M to 1.0 M CH3COOH did not prevent the salt-induced failure. These results demonstrate that operating in the high-SPU, CO2-depleted regime accelerates cell failure through the combined effects of massive (bi)carbonate salt precipitation and the consequent GDE flooding. Accordingly, further operational conditions — increasing the acetic acid humidifier concentration or adopting a stronger-acid humidifier, together with increasing the CO2 flow rate — will be explored to relieve CO2 depletion and extend the operational lifespan of the system.

Figure 3. CO2 electrolysis of 0.5NiSAC (850 °C, 4 h, 10 °C·min−1) / IrO2-TiPt in a 5 cm2 MEA at different applied current densities: (top) FE(CO), FE(H2), SPU, and cell potential after 1 h electrolysis at 100, 200, 250, and 300 mA·cm−2 on a Sustainion AEM; (middle) long-term FE(CO), SPU, and cell voltage at 300 mA·cm−2 and (bottom) at 250 mA·cm−2 comparing 0.5 M and 1.0 M CH3COOH humidifier, both on a PiperION 40 µm AEM. Conditions: 0.5 M CH3COOH humidified CO2 at 20 mL·min−1 (1.0 M for the bottom-panel comparison), 4 mL·min−1 of 0.1 M KHCO3.

Optimization of Ni-SAC catalyst

Effect of pyrolysis temperature and hold time on the surface area, CO2-to-CO selectivity, and durability of 0.5NiSAC

To optimise the 0.5NiSAC synthesis, the effect of pyrolysis temperature (800, 850, and 900 °C) and hold time (2 and 4 h) on the textural properties and CO2RR performance was investigated at a fixed ramp rate of 10 °C·min−1. As shown in Figure 4, the Brunauer–Emmett–Teller (BET) analysis revealed that the pyrolysis temperature directly governed the textural properties: raising the temperature from 800 to 900 °C progressively increased both the specific surface area (135.70 → 171.50 → 181.92 m2·g−1 for the 2 h series and 112.69 → 178.11 → 210.36 m2·g−1 for the 4 h series) and the pore volume (0.34 → 0.41 → 0.52 cm3·g−1 and 0.36 → 0.53 → 0.61 cm3·g−1, respectively). In contrast, extending the hold time from 2 to 4 h exerted only a modest effect on the specific surface area while substantially increasing the pore volume (for example, from 0.41 to 0.53 cm3·g−1 at 850 °C). In terms of CO2RR performance, the 0.5NiSAC synthesised at 850 °C for 4 h (850C-4h-10 °C·min−1) outperformed all other conditions, delivering the highest FE(CO) and the longest operational lifetime. These results indicate that an intermediate pyrolysis temperature combined with the extended 4 h hold time provides the optimal balance of active-site accessibility and mass-transport-favourable porosity for durable CO2-to-CO conversion.

Figure 4. Optimisation of 0.5NiSAC synthesis — effect of pyrolysis temperature and hold time. FE(CO) and cell voltage versus operational time for 0.5NiSAC pyrolysed at 800, 850, and 900 °C for (top) 2 h and (bottom) 4 h at a fixed 10 °C·min−1 ramp rate, with the corresponding BET specific surface area and pore volume tabulated.

Effect of pyrolysis ramp rate on the surface area, CO2-to-CO selectivity, and durability of 0.5NiSAC

To further probe the synthesis parameters, the effect of the heating ramp rate was examined at each pyrolysis temperature, as shown in Figure 5. The BET analysis showed no consistent trend in the textural properties with ramp rate across the temperatures tested: at 850 °C (2 h), increasing the ramp rate from 10 to 20 °C·min−1 raised the specific surface area from 171.50 to 220.90 m2·g−1 with only a marginal change in pore volume (0.41 to 0.43 cm3·g−1), whereas at 900 °C (4 h), increasing the ramp rate from 5 to 10 °C·min−1 slightly lowered both the specific surface area (216.87 to 210.36 m2·g−1) and the pore volume (0.79 to 0.61 cm3·g−1). Consistently, the CO2RR performance exhibited no systematic dependence on ramp rate, with FE(CO) and durability varying inconsistently between conditions. Because the present two-point ramp-rate comparison at each temperature is insufficient to resolve a clear trend, the ramp-rate range will be extended (5, 10, and 20 °C·min−1) to more rigorously establish its effect on the catalyst texture and CO2-to-CO performance.

Figure 5. Optimisation of 0.5NiSAC synthesis — effect of pyrolysis ramp rate at each temperature. FE(CO) and cell voltage versus operational time for 0.5NiSAC pyrolysed at (top) 800 °C / 4 h (5 vs 10 °C·min−1), (middle) 850 °C / 2 h (10 vs 20 °C·min−1), and (bottom) 900 °C / 4 h (5 vs 10 °C·min−1), with the corresponding BET specific surface area and pore volume tabulated.

Upcoming tasks

- 100cm2 MEA electrolyzer operation in 15 position – CO2 electrolysis of 0.5NiSAC (850C-4h-10 C.min-1) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 400 ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 200mA/cm2

- 5cm2 MEA electrolyzer. – CO2 electrolysis of 0.5NiSAC (850C-4h-10 C.min-1) in AEM system at 250mA/cm2: Exploring the possible operational conditions (Effect of CO2 flow rate and acetic acid concentration)