……....................................

Dr. Pongkarn Chakthranont

Project:

Advancing Integrated Materials and Devices for Electrochemical CO2 Reduction (AIM-COR)

Sothearoth Heng (ID: 803198)

Under the supervision of

Dr. Pongkarn Chakthranont

Contract Number: NCR-NN-2026-25421-EN

May 2026 report

May monthly report

- To-do list in May

- Verifying the AgNPs catalyst performance in 5cm2 MEA electrolyzer – CO2 electrolysis of AgNPs (NP size: 50 and 100nm, 0.6mg/cm2) catalysts in AEM system under 0.5M CH3COOH 20ml/min CO2, 4 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2

- 100cm2 MEA electrolyzer – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 200ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2

  - Effect of flow-field configurations on MEA cell performance and durability

  - Influence of CO2 flow rate on long-term stability in parallel flow-field MEA system

- Experimental Procedure

Synthesis of 0.5NiSAC by pyrolysis method

The synthesis of 0.5NiSAC catalyst was followed by our previous work. Initially, nickel phthalocyanine (NiPc), urea, and dicyanamide precursors were stoichiometrically weighed according to mass ratios of 0.5:5:5. Subsequently, the mixture was thoroughly mixed and ground until a homogeneous midnight blue powder was obtained. The fine powder was then transferred into a quartz boat covered with a capsule lid and subjected to polymerization at 800 - 900 °C (ramp rate = 10 °C·min⁻¹) in a horizontal tube furnace under an argon atmosphere (flow rate > 200 sccm) 2 - 4 h.

Preparation of AgNPs cathode via spray coating method

The NiSAC gas-diffusion electrode was fabricated by spray coating onto Sigracet 39BB carbon paper or hydrophilic carbon cloth substrates. Typically, 150 mg of AgNPs and 381 μL of XC-2 ionomer were ultrasonically dispersed in 10 mL of isopropanol (IPA) for at least 1 h to form a homogeneous dark colloidal suspension. The ink suspension was subsequently spray-coated onto a 12 x 12 cm2 carbon substrate using an automated, custom-built spraying setup equipped with a syringe pump operating at a flow rate of 0.6 mL min⁻1 on a hotplate maintained at 130°C, yielding a catalyst mass loading of 0.5 ± 0.1 mg.cm⁻2 AgNPs.

Electrochemical measurements in membrane-electrode assembly (MEA) electrolyzer

5 and 100cm2 MEA electrolyzer operational set-up

A 100 cm2 MEA electrolyzer was used to evaluate the CO2RR performance under modulated operating conditions. The Ni foam or IrO2-TiPt felt (10.5 x 10.5 cm2), bipolar membrane (BPM, 15.6 x 16.8 cm2) or AEM (12 x 12 cm2), and AgNPs (10.5 x 10.5 cm2) were employed as the anode, membrane, and cathode electrode, respectively. The MEA was assembled with 0.25µm PTFE gasket and tightened at a compression force of 8 ft.lb. 10 L of 0.1 M KHCO3 was recirculated and used throughout the experiment as the anolyte at 100 ml/min. The humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 200-1000 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

The 5 cm2 MEA electrolyzer used for evaluating the CO2RR performance and stability of AgNPs in AEM cell configuration, the MEA was assembled with 0.25µm PTFE gaskets with a compression force of 15 in.lbs. 2L of 0.1M KHCO3 anolyte was recirculated at a flow rate of 4ml/min. We refresh the anolyte every 4days of continuous operation to ensure sufficient K+ cation supply and stable pH. The 50mM acetic acid humidified CO2 gas stream was introduced into the cathodic inlet with a total CO2 flow rate of 20 ml/min. Prior the test, the electrochemical impedance spectroscopy (EIS) and Cyclic voltammetry were measured. Meanwhile, the cathodic outlet was directly injected into an online gas-chromatography for gas products analysis.

- Results

Upcoming tasks

- 100cm2 MEA electrolyzer – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 800ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2

- 100cm2 MEA electrolyzer operation in 45 position – CO2 electrolysis of AgNPs (50nm, ~0.6mg/cm2) catalyst in AEM system with 350µm/250µm silicone gaskets and 8 ft.lbs under 50mM CH3COOH humidified 400 or 800 ml/min CO2, 100 ml/min of 0.1M KHCO3, and IrO2-TiPt anode at 100mA/cm2